The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep112ls.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Low Viscosity, Two Component Epoxy is Optically Clear with Non-Yellowing Properties

Master Bond EP112LS is a two part epoxy that is well suited for impregnation, potting, encapsulation, sealing and coating applications, particularly in the aerospace and optoelectronics industries.

EP112LS is optically clear, features reliable non-yellowing properties and has a refractive index of 1.55. This electrically insulative system is resistant to chemicals including water, oils, fuels, acids and bases. EP112LS is serviceable over the temperature range of -60°F to +450°F.

This system features a working life exceeding 2-3 days at room temperature and requires oven curing. Post curing will enhance its properties. With a mixed viscosity of 50-200 cps, EP112LS bonds well to a wide variety of substrates, including metals, composites, glass, ceramics and many rubbers and plastics. Bonds feature a tensile strength, compressive strength and tensile modulus of 11,000 psi, 20,000 psi and 400,000 psi at room temperature, respectively. Dimensional stability is outstanding.

EP112LS has a shelf life of one year in original, unopened containers and is available in ½ pint, pint, quart, gallon and 5 gallon container kits.

Master Bond Electrically Insulative Adhesive Systems

Master Bond 112LS is an optically clear, low viscosity epoxy that has been formulated for a variety of high performance applications. This two component, heat curing system is also a competent electrical insulator, even at elevated temperatures. Read more about Master Bond’s electrically insulative adhesives at http://www.masterbond.com/properties/electrically-insulative-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep112ls

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com