-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep30-2lb.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Optically Clear, Room Temperature Curing Epoxy Blocks UV Light Transmission

Formulated for specific optical applications, Master Bond EP30-2LB blocks UV light from 200-400 nm and allows the transmission of visible light from 450-900 nm. This two part system is optically clear with a refractive index of 1.55. It also passes ASTM E595 testing to meet NASA low outgassing specifications.

Beyond its optical properties, EP30-2LB is a reliable structural adhesive with a tensile lap shear strength of 3,000-3,200 psi and a compressive strength of 14,000-15,000 psi. It bonds well to a wide variety of substrates including metals, composites, glass, ceramics, rubbers and plastics. This epoxy has a ten to one mix ratio by weight and flows smoothly and evenly, enabling it to be used for coating, sealing and encapsulation applications. It is a capable electrical insulator, is dimensionally stable and has low shrinkage upon cure. This material also is easily machineable.

EP30-2LB resists chemicals including water, oils, fuels, acids and bases and many solvents. It is serviceable from -80°F to +300°F [-62°C to +149°C]. This compound has a shelf life of one year at room temperature in its original, unopened containers. It is available for use in ½ pint, pint, quart, gallon and 5 gallon container kits as well as gun dispensers.

Master Bond NASA Low Outgassing Approved Epoxies

Master Bond EP30-2LB offers a unique optical profile that blocks UV light and transmits visible/IR light. This system passes NASA low outgassing tests and offers a high temperature resistance. Read more about Master Bond’s adhesives that pass NASA low outgassing tests at http://www.masterbond.com/certifications/nasa-low-outgassing or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep30-2lb

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #