-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep4s-80 .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Silver Filled, Low Outgassing Epoxy for EMI/RFI Shielding

Master Bond EP4S-80 is a one component silver filled epoxy which meets NASA low outgassing requirements. It has an unlimited working life at room temperature and a moderate heat cure requirement of 80°C. With a viscosity of 10,000-15,000 cps, EP4S-80 has a smooth flow and is easily brushable, making it ideal for EMI/RFI shielding and static dissipation. This formulation can also be used in a variety of applications where electrical conductivity is required: bonding, sealing, coating, as well as gap filling and encapsulating.

EP4S-80 features excellent mechanical properties with a tensile modulus of 500,000-600,000 psi and a compressive strength of 22,000-24,000 psi at 25°C. This electrically conductive system offers a volume resistivity of 0.02-0.06 ohm-cm and a thermal conductivity of 1.30-1.44 W/(m•K). Upon curing, EP4S-80 offers low shrinkage, excellent dimensional stability and a glass transition temperature of 130-135°C. Serviceable over the temperature range of -60°C to +150°C [-75°F to +300°F], this compound adheres well to a variety of substrates such as metals, composites, glass, ceramics, semiconductor materials and many plastics. It is packaged in ounce and pound jars.

Master Bond NASA Low Outgassing Adhesives

Master Bond EP4S-80 is a one part, flowable epoxy system for bonding, sealing, coating, gap filling and encapsulation applications. It meets NASA low outgassing requirements and cures at moderate temperature.  Read more about Master Bond’s NASA low outgassing adhesives at https://www.masterbond.com/certifications/nasa-low-outgassing or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep4s-80

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #