-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep5g-80.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

One Component, Graphite Filled Epoxy Features Electrical and Thermal Conductivity

Master Bond EP5G-80 is a one component, NASA low outgassing rated epoxy, with a moderate temperature cure requirement of 80°C for 4 hours. This graphite filled compound is not premixed and frozen and has an unlimited working life at room temperature. It offers electrical conductivity with a volume resistivity of 5-15 ohm-cm and a thermal conductivity of 2.88-3.46 W/(m•K) at room temperature.

“EP5G-80 is a specialty non-metallic system designed for heat sensitive electronic applications where high levels of conductivity are desired. Its key feature is that it does not need elevated heat to fully cure,” says Rohit Ramnath, Senior Product Engineer. “Unlike other graphite filled adhesives, EP5G-80 is a smooth thixotropic paste and can be easily dispensed manually or using automated systems.”

For a conductive system, EP5G-80 provides an especially high Tg of around 130°-140°C, and a tensile modulus that exceeds 1,000,000 psi at room temperature. It is serviceable over the temperature range of -50°C to +175°C and has a low coefficient of thermal expansion. Suitable for bonding, sealing and coating, EP5G-80 adheres well to a variety of substrates such as metals, composites, ceramics and many plastics. This formulation features a good lubricity and can be employed for static dissipation and EMI/RFI shielding applications. It is black in color and RoHS compliant. Packaging is available in syringes, jar and pint containers.

Master Bond Thermally Conductive Epoxies

Master Bond EP5G-80 is a one part, non-premixed and frozen epoxy system used for bonding, sealing and coating. This graphite filled system exhibits high electrical and thermal conductivity and meets NASA low outgassing requirements. It is syringe dispensable, can cure at temperatures as low as 80°C and provides excellent heat resistance. Read more about Master Bond’s thermally conductive adhesives at https://www.masterbond.com/properties/thermally-conductive-epoxy-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep5g-80

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #