____________________________________________________________________________

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep70cn  .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

High Tensile Strength Epoxy Adhesive Utilizes Renewable Biomaterial

Master Bond EP70CN is a two part, thermally stable epoxy adhesive formulated using a natural, renewable and sustainable ingredient. This epoxy system forms high physical strength bonds and can be utilized for bonding, sealing, coating and potting. “The tensile strength is 11,000 to 12,000 psi and the tensile modulus, 300,000 to 350,000 psi. It features a glass transition temperature of 130 to 135°C”, says Rohit Ramnath, Senior Product Engineer. “The EP70CN has a very good chemical resistance profile when cured at the optimal cure schedule.”

It is a low viscosity formulation with a mixed viscosity of 2,500 to 5,000 cps. With a long working life of 60 to 90 minutes and a variety of curing options, the optimal cure schedule is overnight at room temperature followed by 3-4 hours at 140°F to 170°F. EP70CN bonds well to a wide variety of substrates including metals, ceramics and many rubbers, plastic materials, and especially composites with low shrinkage upon cure. It features excellent wetting properties which makes it suitable for applications involving bonding and sealing fibers. EP70CN has a high volume resistivity (greater than 1014 ohm-cm) and a relatively low exotherm. This combination of properties enables it to be used in many encapsulating applications.

EP70CN can be used in aerospace, electronic, opto-electronic and OEM applications, particularly those involving composites and fibers. In addition to specialty packaging in the form of premixed & frozen syringes and FlexiPaks®, EP70CN is available in standard packaging of ½ pint, pint, quart and gallon kits.

Master Bond Chemically Resistant Adhesive Systems

Master Bond EP70CN is a two component epoxy system for bonding, sealing, coating and potting featuring a natural curing agent. It withstands many chemicals, including solvents, fuels and bases. Read more about Master Bond’s chemically resistant adhesives at https://www.masterbond.com/properties/chemical-resistance  or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep70cn

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #