The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/mastersil-980.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Two Part, Addition Cured Fluorosilicone Offers Excellent Chemical Resistance

Master Bond MasterSil 980 is two part fluorosilicone system for high performance bonding, sealing, coating and potting applications. It withstands harsh chemicals such as gasoline, diesel fuel, motor oil, ethanol and many solvents. After testing, chemical resistance for MasterSil 980 was far superior when compared to standard type silicone systems.

With an elongation of 100-200% at 75°F, this fluorosilicone offers enhanced flexibility while maintaining resistance to aggressive thermal cycling and mechanical shock. It features a wide service temperature range from -85°F to +465°F. MasterSil 980 bonds well to a wide variety of substrates including metals, composites, ceramics, glass, rubbers, plastics as well as other silicones. This electrically insulative material has a dielectric constant of 6.4 (measured at 75°F, 60Hz) and a volume resistivity of more than 1014 ohm-cm.

Upon mixing, MasterSil 980 yields a moderate viscosity with good flow and a user friendly open time of 6-9 hours at room temperature for a 50 gram batch. As an addition cured system, it does not require air or humidity for cross-linking. It cures well in deep and wide sections making it ideal for use in various potting and encapsulation applications. With a hardness of 20-30 Shore A, it is also well suited for formed-in-place gasketing. MasterSil 980 can be utilized across many industries including aerospace, specialty OEM and chemical processing among others.

Master Bond Chemical Resistant Adhesives

MasterSil 980 is a flexible, two part fluorosilicone with high temperature resistance. This system easily withstands a wide variety of aggressive chemicals, even after prolonged exposure. Read more about Master Bond’s chemical resistant polymer adhesives at https://www.masterbond.com/properties/chemical-resistance or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/mastersil-980

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #