-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/mastersil-151s.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Silver Conductive Silicone Adhesive Meets NASA Low Outgassing Specifications

Master Bond MasterSil 151S is an addition curing two part silicone system that may be used as an adhesive, sealant, coating or form-in-place gasketing material. A unique feature of this product is that despite its silicone chemistry, it passes NASA low outgassing specifications. Also, it retains superior electrical conductivity with a volume resistivity of 0.004 ohm-cm at 75 °F. “This silicone is ideal for applications where low stress is required, since it is highly flexible across a wide service temperature range. It is capable of resisting aggressive thermal cycles and shocks,” says Rohit Ramnath, Senior Product Engineer.

The mix ratio of MasterSil 151S is 100 to 5 by weight, and it cures with the addition of heat. Upon mixing, it retains its smooth, paste consistency, and has a long working life of 6-12 hours for a 50 gram mass. This silicone product has an elongation between 100-150%, tensile strength of 400-700 psi and can cure beyond ¼ inch thick. It features a thermal conductivity of 1.30-1.59 W/(m•K), a  coefficient of thermal expansion of 150-200 x 10-6 in/in/°C, and hardness of 80-90 Shore A. It is serviceable over the temperature range of -80°F to +400°F.

This compound bonds well to a variety of substrates including metals, ceramics, composites and many plastics and rubbers. It is available for use in 20 gram, 50 gram and 100 gram glass jars. The color of Part A is silver and Part B is clear. MasterSil 151S has a low linear shrinkage upon curing and is RoHS compliant.

Master Bond Electrically Conductive Adhesive Systems

Master Bond MasterSil 151S is a two part, electrically conductive silicone that passes NASA low outgassing requirements. This silver filled, highly flexible system can be used for low stress applications. Read more about Master Bond’s electrically conductive adhesives at https://www.masterbond.com/properties/electrically-conductive-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/mastersil-151s

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #