-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/uv15-42c.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Optically Clear UV Curable System Offers High Bond Strength and Fast Cures

Specially formulated to optimize bond strength, Master Bond UV15-42C is a UV curable system for bonding, sealing and coating applications. This smooth paste can be applied vertically without sagging. As an optically clear compound, it is often used in the fiber-optic, optical, electronic, aerospace and specialty OEM industries.

This one part system bonds well to a wide variety of substrates including glass, metals, composites, rubbers and most plastics. Adhesion to acrylic and polycarbonates is exceptional. UV15-42C also features a tensile strength of 5,000-6,000 psi and a tensile modulus of 250,000-300,000 psi at room temperature. Its toughness enables it to withstand thermal cycling as well as mechanical shock. UV15-42C is also resistant to chemicals such as water, oils, cleaning agents, acids and bases.

It cures readily in 10-30 seconds upon exposure to a UV light source emitting a 320-365 nm wavelength with an energy output of 20-40 milliwatts/cm2. UV15-42C is not oxygen inhibited and will cure in thicknesses up to ¼ inch. This electrically insulative, dimensionally stable system has low shrinkage upon curing.

UV15-42C is serviceable from -65°F to +300°F and is available for use in syringes and cartridges. It can also be purchased in ½ pint, pint and quart containers.

Master Bond Non-Drip Adhesives

Master Bond UV15-42C is an optically clear, toughened, UV curing system that bonds well to many substrates. This one part formulation is easy to handle with a non-sagging paste viscosity and rapid cures. Read more about Master Bond’s non-drip adhesives at http://www.masterbond.com/properties/non-drip-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/uv15-42c

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #