The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/uv26.

-----------------------------------------------------------------

FOR IMMEDIATE RELEASE

NASA Low Outgassing Rated UV Curing Adhesive with High Glass Transition Temperature

Master Bond UV26 is a new one part UV curable system featuring an exceptionally high glass transition temperature (Tg) ranging from 160 to 170°C. This NASA low outgassing certified compound also offers strong adhesion to a wide variety of substrates such as glass, surface treated metals and many plastics. As a coating and adhesive it is also capable of withstanding harsh chemicals including acids, bases, fuels and many aggressive solvents.

This low viscosity compound (250-1,500 cps at 75°F) cures rapidly upon exposure to a UV light source at a wavelength of 320-365 nm with an energy output as low as 20-40 milliwatts per cm2. With a refractive index of 1.55 at room temperature, this system features outstanding optical clarity. UV26 offers robust physical strength properties upon curing and is ideal for high performance bonding and coating applications. It features low shrinkage upon curing and serviceability from -60°F to +500°F [-51°C to +260°C].

Master Bond UV26 is 100% solids, does not contain any solvents or volatiles and is not oxygen inhibited. It is available for purchase in 10 cc and 30 cc syringes, ½ pint and 1 pint containers. The shelf life at 75°F is 6 months in the original unopened containers.

Master Bond Adhesives with High Tg

Master Bond UV26 offers the convenience of a no mix system and rapid cures upon exposure to a UV light source. It features low outgassing properties and excellent chemical resistance while maintaining superb physical strength, even upon exposure to high temperatures. Read more about Master Bond’s high glass transition temperature formulations at https://www.masterbond.com/properties/epoxy-adhesive-systems-high-glass-transition-temperature or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/uv26

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #