Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  This email was sent to (%email%)

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/newsrelease/ep15.

----------------------------------

FOR IMMEDIATE RELEASE

One Part Epoxy Offers Exceptionally High Tensile Strength

HACKENSACK, NJ – February 23, 2012 – Primarily used for testing the adhesion or cohesive strength of flame sprayed coatings as per the ASTM C633 specification, Master Bond EP15 produces high strength bonds across a wide variety of applications. This one component epoxy bonds well to many similar and dissimilar substrates. Particularly noteworthy is its adhesion to metals and ceramics.

Featuring a tensile strength exceeding 12,000 psi at room temperature, this 100% reactive system offers superior dimensional stability with minimal shrinkage upon cure. It is serviceable from -60°F to 250°F. EP15 has superior chemical resistance properties and withstands thermal cycling.

As a one part system, EP15 features an unlimited working life and does not require any mixing prior to use. This system offers good flow properties with a viscosity of 40,000-65,000 cps and can be easily applied with a brush, paint roller or spatula. It cures quickly in 60-90 minutes at 300-350°F.

The standard color for this epoxy is tan and it is available in many sizes, including 1/2 pint, pint, quart, gallon and 5 gallon containers. Master Bond EP15 has a minimum shelf life of 3 months when stored in original, unopened containers.

- Master Bond High Strength Adhesives

Master Bond EP15 offers exceptional tensile strength and was developed for ASTM C633 specification testing. This no mix epoxy adhesive has versatile, rapid cure schedules. Read more about Master Bond’s high strength adhesives at http://www.masterbond.com/properties/high-shear-strength-adhesives or contact Technical Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: Technical@masterbond.com.

- CONTACT:

- James Brenner, Marketing Manager

- Email: jbrenner@masterbond.com

- Tel: +1-201-343-8983

Fax: +1-201-343-2132

- MASTER BOND INC.

- 154 Hobart Street

Hackensack, NJ 07601-3922

- Web: www.masterbond.com

# # #