This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep21ar.

----------------------------------

FOR IMMEDIATE RELEASE

Chemically Resistant Epoxy Withstands 
a Year in Sulfuric & Hydrochloric Acid!

HACKENSACK, NJ – March 1, 2011 – For applications demanding exceptional chemical resistance, especially to acids, fuels, and oils, Master Bond has developed EP21AR.  Whether coating, lining, bonding or sealing, this two-component epoxy can withstand harsh, acidic environments, including prolonged immersion in 96-98% sulfuric acid and 36% hydrochloric acid for over a year.

With a dielectric strength of 400 volts/mil, EP21AR is a durable and stable epoxy that is also a superb electrical insulator. Its coefficient of thermal expansion is 45-55 ppm/°C, and it is serviceable from -60°F to +275°F. It produces high strength, abrasion resistant bonds with a tensile strength over 10,000 psi, a shear strength exceeding 2,700 psi, and a compressive strength greater than 14,000 psi at 75°F.

EP21AR is easy to use with a forgiving 2 to 1 mix ratio by weight, and a mixed viscosity of 10,000-15,000 cps. It is 100% reactive with no solvents or diluents and can be applied smoothly in any thickness. This epoxy has a working life of 45 to 55 minutes at ambient temperature for a 200 gram batch, and cures at room temperature or faster at elevated temperatures. It bonds well to a wide variety of substrates, including metals, glass, ceramics, cements, vulcanized rubbers, wood and many plastics.

EP21AR is packaged in pint, quart, gallon and 5 gallon container kits. It is widely used in an array of industries, including oil and chemical processing, maintenance and repair, optics, metalworking, appliance, and electrical/electronic.

Master Bond Chemically Resistant Adhesives

Master Bond EP21AR is ideal for applications that require high strength, electrically insulative bonds in an acidic or corrosive environment. Read more about Master Bond’s Chemically Resistant Epoxies at http://www.masterbond.com/lp/tabs/tp_pp_chemresist.html or contact Technical Support by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at technical@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #