This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep21lv.

----------------------------------

FOR IMMEDIATE RELEASE

Low Viscosity, Room Temperature Curing Epoxy 
Complies With FDA and USP Class VI Requirements

HACKENSACK, NJ – June 9, 2011 – Ideal for potting and encapsulation applications, Master Bond EP21LV features a low viscosity and outstanding electrical insulation properties. It is broadly used in the medical and food industries, as it conforms to USP Class VI and Title 21, U.S. Code of Federal Regulations, FDA Chapter 1, Section 175.105 requirements.

Offering a forgiving 1 to 1 mix ratio by weight or volume, EP21LV cures at room temperature in 24 to 36 hours or faster at elevated temperatures. This system is unique in that the rigidity of its cure can be altered by adjusting its mix ratio. For example by adding more of Part A (for example, in a 2 to 1 ratio), users will get a more rigid cure with enhanced machinability. Switching to a 1 to 2 mix ratio yields a more forgiving cure with improved impact resistance.

Serviceable over the wide range of -65°F to +250°F, this epoxy features a long working life of 60 to 75 minutes for a 200 gram mass. EP21LV bonds well to a variety of substrates including metals, glass, wood, rubbers, ceramics and many plastics. It resists thermal cycling as well as water, oils, fuels, bases, acids and salts. EP21LV produces durable bonds with a tensile strength of 7,600 psi, a shear strength over 2,900 psi and an elongation of 4.8% at 75°F. This versatile two-component epoxy has a volume resistivity of 1015 ohm-cm and a coefficient of thermal expansion of 53 in/in x 10-6/ °C.

In addition to its standard amber-clear color, EP21LV is available in a wide variety of alternative colors. Parts A and B come in pint, quart, gallon and five gallon container kits.

Master Bond Electrically Insulative Epoxy Resin Systems

Developed for high performance bonding, sealing, coating, encapsulation, and casting, Master Bond’s EP21LV combines exceptional electrical insulation properties with a low viscosity. Read more about Master Bond’s electrically insulative epoxies at http://www.masterbond.com/lp/tabs/tp_pp_elecinsulative.html or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #