This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep30p.

----------------------------------

FOR IMMEDIATE RELEASE

Low Viscosity Epoxy Features Excellent Adhesion
to Glass, Polycarbonates & Acrylics

HACKENSACK, NJ - Dec 7, 2006 -- Master Bond Inc has introduced EP30P, a new two component, transparent, low viscosity epoxy system for high performance bonding, sealing, coating, encapsulation and casting.  This system has a 4 to 1 mix ratio by weight and is formulated to cure at room temperatures.  Cures can be accelerated by the use of heat.  EP30P bonds well to a wide variety of substrates including metals, glass, ceramics and many plastics.  It has a service operating temperature range of -60°F to +250°F.

Master Bond EP30P is a 100% reactive system and contains no solvents or diluents.  It has exceptionally low linear shrinkage upon cure and offers outstanding electrical insulation properties.  It forms bonds that are rigid and have high strength. Tensile strength is >9500 psi.  EP30P also exhibits superior resistance to water, acids, bases and salts.

Master Bond EP30P is easy to apply.  It has a mixed viscosity of 1,200-1,400 cps.  It is available in pint, quart, gallon and 5 gallon container kits.  It can also be applied with a convenient gun applicator.  Shelf life at 75°F is 6 months in original unopened containers.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #