----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  If you do not wish to receive news releases from us or you are not the proper contact for news releases please email us at newsrelease@masterbond.com.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.

----------------------------------

FOR IMMEDIATE RELEASE

High Temperature Resistant Epoxy Has Exceptional Thermal Conductivity

HACKENSACK, NJ - Sep 15, 2004 -- Master Bond Inc. of Hackensack, New Jersey has introduced a new high performance, room temperature curing, two component epoxy adhesive/sealant called EP34AN.  This compound features a thermal conductivity of 22-24 BTU/in/ft²/hr/°F.  Physical properties are maintained even after long exposure to temperatures in the 400-450°F range.  EP34AN has superb dimensional stability and a low coefficient of expansion.  It also exhibits superior electrical insulation properties.

Master Bond EP34AN has a 100 to 70 mix ratio by weight.  It is easy to mix and can be applied without sagging or dripping even on vertical surfaces.  The adhesive/sealant spreads smoothly and only contact pressure is required for cure.  It is 100% reactive and does not contain any solvents or diluents.  Cures can be accelerated by the use of heat.

EP34AN has high bonding strength to a wide range of substrates.  Adhesion to metals, glass, ceramics, wood, vulcanized rubbers and most plastics is excellent.  Additionally, EP34AN is resistant to thermal shock and many chemicals including water, oil and most organic solvents.  It has a Shore D hardness of >85 and a tensile strength of 5,500 psi.  Its tensile modulus is >500,000 psi.

Master Bond EP34AN is available for use in pint, quart, gallon and 5 gallon container kits.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #