This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr= ep37-3flf.

----------------------------------

FOR IMMEDIATE RELEASE

Optically Clear, Highly Flexible Epoxy Cures at Room

Temperature and Withstands Cryogenic Conditions

HACKENSACK, NJ – March 24, 2011 – For demanding applications where highly flexible, impact resistant bonds are required, Master Bond developed Polymer System EP37-3FLF. This optically clear, two component epoxy has exceptional resistance to cryogenic temperatures and severe thermal cycling.  Its low exotherm also makes it a superb potting, encapsulating and casting system, especially where wider cross section thicknesses are specified. Its unique combination of properties allows it to cure without stressing delicate electronic components.

Serviceable over the wide range of 4K to 250°F, EP37-3FLF cures at room temperature in 2 to 3 days or faster at elevated temperatures. This epoxy offers a convenient, non-critical 1 to 1 mix ratio by weight or volume, and a low mixed viscosity of 1,400 to 1,500 cps. Additionally, users can work with a 100 gram mass of the adhesive at room temperature for up to 90 minutes.

EP37-3FLF has a bond shear strength exceeding 2,000 psi and a T-peel strength of 25 pli. This flexible epoxy has an elongation of 180% and superior electrical insulation properties with a volume resistivity of 1x1014 ohm-cm. It bonds well to a variety of substrates including metals, glass, ceramics, rubbers and many plastics and is widely used in the optical, electrical, electronic, computer and OEM industries.

EP37-3FLF is sold in pint, quart, gallon and 5 gallon container kits and has a 6 month shelf life if unopened and stored at room temperature.

Master Bond Low Stress Epoxies

Master Bond’s EP37-3FLF is a highly flexible, room temperature curing epoxy designed for high performance applications in many industries across a wide service temperature range. Read more about Master Bond’s low stress epoxies at http://www.masterbond.com/lp/tabs/tp_pp_lowstress.html or contact Technical Support by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #