----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  If you do not wish to receive news releases from us or you are not the proper contact for news releases please email us at newsrelease@masterbond.com.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.

----------------------------------

FOR IMMEDIATE RELEASE

One Component Silver Conductive Adhesive System

Meets NASA Outgassing Test Requirements

HACKENSACK, NJ - Jan 30, 2003 -- Master Bond Polymer System Supreme10HT/S is a uniquely formulated silver filled one component epoxy compound with an unsurpassed wide service temperature range from cryogenic service temperatures up to as high as 400°F.  This remarkably versatile electrically conductive epoxy composition features high physical strength properties, superior chemical resistance and excellent durability even when exposed to various severe environmental conditions. Additionally it fully meets NASA low outgassing requirements.

Supreme 10HT/S has a shelf life of 3 months at ambient temperatures.  The shelf life can be readily extended by storage at lower temperatures.  No mixing is needed for use. Cure can be effected by heating at 250°F for approx. 1 hour or 300°F for 30 minutes, less at higher temperatures.  A snap cure version called Supreme 10HTSF is available which will cure at 380-400°F in less than 2 minutes. Supreme 10HT/S has excellent bonding properties. Lap shear strengths with properly prepared substrates exceed 1800psi and peel strengths are impressively high.  Master Bond Supreme 10HT/S has been acclaimed for outstanding resistance to thermal cycling, mechanical shock and vibration.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #